CENELEC European Committee for Electrotechnical Standardization（欧洲市场统一标准电源线） 
Approval No: 40020058
	PRODUCT DESCRIPTION（说明）

	H03VVH2-F & H03VV-F

	Bare stranded copper condutor
	导体使用裸软铜绞线

	Color-coded PVC insulation and jacket
	PVC绝缘及被覆

	Rated temperature: +70℃ 
	额定温度：+70℃

	Rated voltage: 300/500 vlots
	额定电压：300/500V

	H05VVH2-F & H05VV-F

	Bare stranded copper condutor
	导体使用裸软铜绞线

	Color-coded PVC insulation and jacket
	PVC绝缘及被覆

	Cores twisted together 
	芯线绞合

	Rated temperature: +70℃ 
	额定温度：+70℃

	Rated voltage: 300/500 vlots
	额定电压：300/500V

	APPLICATIONS（应用）

	Suitable for indoor small electrical instruments. 
	适用于小型室内器具、家电产品电力供应线

	CONSTRUCTION（构造）

	[image: image1.jpg]Copper Conductor
PVC insulation PVC ##

——PVC jacket PVC # 8




[image: image2.jpg]—————— Copper Conductor ¥

E ——————PVCinsulation PVC f:#k

PVC jacket PVC # 8



 

	UL Style 
& 
CSA Type

Conductor 导体

Insulation 
Thickness 
绝缘厚度

Jacket

Max. Cond. Resist. 

Area

Construction

Diam. of Single

被覆体

(mm square)

No./mm

(mm)max

Nom. Thick.(mm)

Nom. Thick.(mm) 

Diam.(mm)

ohm/km(20℃)

截面积

结构

单支线径

厚度

厚度

完成外径

最大导体电阻

H03VVH2-F

2×0.75

24/0.20

0.21

0.5

0.6

3.5×5.5

26.0

H03VV-F

2×0.75

24/0.20

0.21

0.5

0.6

5.5

26.0

3G0.75

24/0.20

0.21

0.5

0.6

6.0

26.0

H05VVH2-F

2×0.75

24/0.20

0.21

0.6

0.8

4.0×6.3

26.0

H05VV-F

2×0.75

24/0.20

0.21

0.6

0.8

6.5

26.0

2×1.0

32/0.20

0.21

0.6

0.8

6.7

19.5

2×1.5

30、0.254

0.26

0.7

0.9

8.0

13.3

3G0.75

24/0.20

0.21

0.6

0.8

6.8

26.0

3G1.0

32/0.20

0.21

0.6

0.8

7.0

19.5

3G1.5

30/0.254

0.26

0.7

0.9

8.5

13.3



	Contact us...（联系方式）

	Florence: florence@126.com
Tom: oasiselectronics@yahoo.cn

	 


